## Slide 1: Organometallic Precursors for the Deposition of Inorganic Materials
Lisa McElwee-White
Department of Chemistry
University of Florida

## Slide 2
Where we are…
University of Florida
(Site for student secondments)

## Slide 3: What Do We Do?
We are organometallic chemists.
We synthesize new complexes, elucidate reaction mechanisms, perform electronic structure calculations, determine structure-reactivity relationships, etc.
We design precursors for deposition of materials….
….tailored for several different techniques
We do interdisciplinary work with lots of collaborators in chemistry, chemical engineering, materials science, electrical engineering, etc.

## Slide 4: Projects
Design and synthesis of precursors for:
EBID of metal nanostructures
CVD of metal nitride films as diffusion barriers for integrated circuits
CVD of metal oxide films as hole injection layers for OLEDs
Photoassisted CVD for metallization on thermally sensitive organic electronics
Surface plasmon mediated deposition of nanostructures

## Slide 5: EBID of metal nanostructures
Collaborative work with Howard Fairbrother (Johns Hopkins Chemistry)
Oddur Ingólfsson (University of Iceland)
and Ivo Utke (EMPA)

## Slide 6: Precursor Development: cis-Pt(CO)2Cl2
Belli Dell’ Amico et al, J. Chem. Soc., Dalton Trans., 1996, 4317.
White/light yellow needles
Extreme sensitivity to moisture
Stable under CO in the freezer for months
Sublimes under vacuum
IR: nCO 2127, 2171 cm-1
13C NMR: d 151.84
Synthesis
Characterization
Properties

## Slide 7
Electron
Source
e-
Substrate (~295 K)
Gas Injection System
hn
e-
Substrate ( < 200 K)
e-
e-
e-
e-
X-ray
Source
MS
Electron
Source
Energy
Analyzer
< 10-8 Torr
Typical EBID Experiment
Constant partial pressure of precursor
Substrate at room temperature
Focused electron beam (20 – 200 KeV)
Size scale: ~ nm3
Analytical techniques: SEM, EDX
Information obtained: composition and
dimensions of deposited structure
~10-5 Torr
UHV Surface Science Approach
Screening by UHV Surface Science
Graphic (and Experiments): Howard Fairbrother
Fixed initial coverage of precursor molecules
Substrate cooled to < 200K
Defocused low energy electron beam (0.5 KeV)
Size scale: ~ cm2
Analytical techniques: XPS, MS
Information obtained: kinetic and mechanistic
details of precursor decomposition

## Slide 8
Screening by UHV Surface Science: cis-PtCl2(CO)2
e-
Spencer, Wu, McElwee-White, Fairbrother, J. Am. Chem. Soc., 2016, 138, 9172.

## Slide 9: CVD of metal nitride films as diffusion barriers for integrated circuits
Collaborative work with Tim Anderson (UF/UMass Chemical Engineering)
CVD of metal oxide films as hole injection layers for Organic Light Emitting Diodes (OLEDs)
Collaborative work with Tim Anderson (UF/UMass Chemical Engineering)
and Roman Korotkov (Arkema, Inc)

## Slide 10: Screening of CVD Precursors
by thermogravimetric analysis
by mass spectrometry
by NMR kinetics
by X-ray crystallography
by DFT calculations
1a
2a
3a
+ H2
+ H2
- HCl
- HCl
36.1
kcal/mol
36.3
-23.4
-23.3
+ H2
- HCl
37.1
-23.8
MI-1
TS-1
TS-2
TS-3

## Slide 11: Photoassisted CVD for metallization on organic electronics
Collaborative work with Amy Walker (UT Dallas)

## Slide 12: Precursor Development: CpRu(CO)2Me
Desired precursor characteristics for deposition on patterned SAMs:
Volatile
High quantum yields for ligand loss
Potential for ligands to react with protic surface
                Sublimes at 50 °C at 1 atm
                Φ = 0.4 for loss of CO
                Methyl could react with –COOH or –OH terminated SAMs
Johnson, Arevalo Rodriguez, Brewer, Brannaka, Shi, Yang, Salazar, McElwee-White, Walker, J. Chem. Phys., under revision.

## Slide 13: Current Research Group
11 PhD students
5 undergraduates